Chapter 10 - Powder Methods of Change of Form

Power metallurgy - the process of compacting metal powders in suitable dies and sintering them.

- Net shape parts of fairly complex shape can be produced economically

- Competitive with casting, forging and machining

- Good dimensional accuracy and size; from balls for ball point pens to parts weighing 200 lbs.

- Parts such as

  - Self lubricating bearings impregnated with oil

  - Break pads with embedded ceramic fibers

  - Machine tool cutting instruments; cermets (ceramic-metals) higher heat absorption

  - Commonly made out of iron, copper, aluminum, tin, and nickel

Order of operation: Powder production, blending, compacting, sintering, finishing

- Powder Preparation

  - Crushing – Ball mill is used to reduce brittle material such as ceramic and glass into a powder.

  - Grinding - Metal can be ground under a water spray or in an inert gas atmosphere so that it does not oxidize.

  - Plating - Plating it onto a temporary surface then scraping it off.

  - Atomization - melt dropped through a hole with an inert gas blown through it to form powder.

Screening - separation of power into certain sizes. Too small particles may be difficult to handle, too large of particles may not display the desired structures.

- Blending - mixing several powders of different sizes, a dry lubricant or an antioxidant for uniform compaction. (done carefully to avoid explosions)

- Can add lubricants- do not stick to mold walls

- Can add binders- so green strength is adequate

- Can add sintering aids- acceleration of densification upon heating

- Compaction- bringing the materials into required shape

Briquetting - Compression of powder in the die cavity from both the top and the bottom.

Roller Compaction - compacted between two rollers to produce sheet or plate stock.

Extrusion Compacting - powder packed into a mild steel tube, then forced through a die.

- Sintering - the process of heating compressed powdered metals to below its melting point but high enough to allow bonding of individual particles.

- Used for materials such as ceramics and cermets that cannot be melted and cast by other methods.

- Finishing of Sintered Parts

Infiltration - Because powder-formed parts can be very porous, other materials can be placed in the voids to enhance the properties of the product.

  - Prevents moisture penetration

  - Lowers frictional properties

Impregnation - Impregnating the sintered part with oil to create a “self lubricating” bearing.

Sizing - forcing the part through a finish die to provide dimensional accuracy

Advantages

  - Wide range of mech. & phys. properties

  - Parts made from high melting point metals

  - High production rates on relatively complex parts

  - Good dimensional control

  - Impregnating and infiltration

Limitations

  - Size of parts, complexity of shapes of parts

  - High cost of powdered metal compared to other materials

  - High tooling cost for small production runs

  - Lower strength and ductility than forging